|  |
| --- |
| **SAE AS22759/190** |

|  |  |
| --- | --- |
|  | * M22759/190 is a lightweight, high performance aerospace hook-up wire insulated with a layer of polytetrafluoroethylene (PTFE) tape/polyamide/PTFE tape, covered with PTFE tape that has been fused to create a seamless jacket. These wires are designed for aerospace and other applications requiring thermal stability, lightweight and high break strength. |
| |  |  | | --- | --- | | Conductor: | Nickel Plated High Strength Copper Alloy | | Insulation: | PTFE/polyimide/PTFE tape and PTFE tape | | Temp Rating: | 260°C | | Voltage Rating: | 600 Volts R.M.S. | | M27500 Type: | DN | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Insulation Diameter**  **Min. Max.** | | **LBS/MFT** |
| **BSPW-26020-X** | 26 | 19 x 38 | 0.033 | 0.037 | 1.55 |
| **BSPW-26030-X** | 24 | 19 x 36 | 0.038 | 0.042 | 2.15 |
| **BSPW-26040-X** | 22 | 19 x 34 | 0.043 | 0.047 | 3.00 |
| **BSPW-26050-X** | 20 | 19 x 32 | 0.051 | 0.055 | 4.55 |

X = Color: See Page BCC-1

|  |
| --- |
| **SAE AS22759/191** |

|  |  |
| --- | --- |
|  | * M22759/191 is a lightweight, high performance aerospace hook-up wire insulated with a layer of polytetrafluoroethylene (PTFE) tape/polyamide/PTFE tape, covered with PTFE tape that has been fused to create a seamless jacket. These wires are designed for aerospace and other applications requiring thermal stability, lightweight and high break strength. |
| |  |  | | --- | --- | | Conductor: | Silver Plated Copper | | Insulation: | PTFE/polyimide/PTFE tape and PTFE tape | | Temp Rating: | 200°C | | Voltage Rating: | 600 Volts R.M.S. | | M27500 Type: | DP | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Insulation Diameter**  **Min. Max.** | | **LBS/MFT** |
| **BSPW-27020-X** | 26 | 19 x 38 | 0.030 | 0.034 | 1.43 |
| **BSPW-27030-X** | 24 | 19 x 36 | 0.034 | 0.038 | 1.93 |
| **BSPW-27040-X** | 22 | 19 x 34 | 0.040 | 0.043 | 2.85 |
| **BSPW-27050-X** | 20 | 19 x 32 | 0.048 | 0.051 | 4.38 |
| **BSPW-27060-X** | 18 | 19 x 30 | 0.056 | 0.060 | 6.6 |
| **BSPW-27070-X** | 16 | 19 x 29 | 0.063 | 0.067 | 8.3 |
| **BSPW-27080-X** | 14 | 19 x 27 | 0.076 | 0.080 | 12.6 |
| **BSPW-27090-X** | 12 | 37 x 28 | 0.096 | 0.100 | 19.6 |
| **BSPW-27000-X** | 10 | 37 x 26 | 0.119 | 0.123 | 30.6 |

X = Color: See Page BCC-1