|  |
| --- |
| **M16878/4 CABLE - SHIELDED, EXTRUDED FEP JACKET** |

|  |  |
| --- | --- |
| Macintosh HD:Users:martinweiner1:Desktop:download.jpeg | PTFE insulated conductors (Type E - MIL-W-16878/4), color coded, cabled for 2 or more conductors, braided with silver-plated copper (90% minimum coverage), with an extruded FEP overall jacket. |
| |  |  | | --- | --- | | Conductor: | Silver Plated Copper | | Insulation: | Extruded PTFE | | Jacket: | Extruded FEP | | Temp Rating: | 200°C | | Voltage Rating: | 600 Volts R.M.S. | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Number of Conductors** | **Nom. O.D. Over Conductor Inches** | **Finished Cable Nominal O.D. Inches** |
| **BCB-9671XE** | 16 | 19/29 | 1 | 0.053 | 0.120 |
| **BCB-9672XE** | 16 | 19/29 | 2 | 0.053 | 0.203 |
| **BCB-9673XE** | 16 | 19/29 | 3 | 0.053 | 0.215 |
| **BCB-9674XE** | 16 | 19/29 | 4 | 0.053 | 0.235 |
| **BCB-9675XE** | 16 | 19/29 | 5 | 0.053 | 0.250 |
| **BCB-9676XE** | 16 | 19/29 | 6 | 0.053 | 0.270 |
| **BCB-9681XE** | 14 | 19/27 | 1 | 0.067 | 0.135 |
| **BCB-9682XE** | 14 | 19/27 | 2 | 0.067 | 0.233 |
| **BCB-9683XE** | 14 | 19/27 | 3 | 0.067 | 0.248 |
| **BCB-9684XE** | 14 | 19/27 | 4 | 0.067 | 0.272 |
| **BCB-9685XE** | 14 | 19/27 | 5 | 0.067 | 0.300 |
| **BCB-9686XE** | 14 | 19/27 | 6 | 0.067 | 0.320 |
| **BCB-9691XE** | 12 | 19/25 | 1 | 0.084 | 0.154 |
| **BCB-9692XE** | 12 | 19/25 | 2 | 0.084 | 0.271 |
| **BCB-9693XE** | 12 | 19/25 | 3 | 0.084 | 0.290 |
| **BCB-9694XE** | 12 | 19/25 | 4 | 0.084 | 0.319 |

Cable Configurations up to 10 conductors.

\*Jackets can be made in all colors.