|  |
| --- |
| **M16878/4 CABLE - SHIELDED, PTFE TAPE JACKET** |

|  |  |
| --- | --- |
|  | PTFE insulated conductors (Type E - MIL-W-16878/4), color coded, cabled for 2 or more conductors, braided with silver-plated copper (90% minimum coverage), with a PTFE Teflon® tape overall jacket. |
| |  |  | | --- | --- | | Conductor: | Silver Plated Copper | | Insulation: | Extruded PTFE | | Jacket: | PTFE Tape | | Temp Rating: | 200°C | | Voltage Rating: | 600 Volts R.M.S. | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Number of Conductors** | **Nom. O.D. Over Conductor Inches** | **Finished Cable Nominal O.D. Inches** |
| **BCB-9621TJ** | 26 | 19/38 | 1 | 0.019 | 0.077 |
| **BCB-9622TJ** | 26 | 19/38 | 2 | 0.019 | 0.121 |
| **BCB-9623TJ** | 26 | 19/38 | 3 | 0.019 | 0.127 |
| **BCB-9624TJ** | 26 | 19/38 | 4 | 0.019 | 0.137 |
| **BCB-9631TJ** | 24 | 19/36 | 1 | 0.024 | 0.086 |
| **BCB-9632TJ** | 24 | 19/36 | 2 | 0.024 | 0.129 |
| **BCB-9633TJ** | 24 | 19/36 | 3 | 0.024 | 0.136 |
| **BCB-9634TJ** | 24 | 19/36 | 4 | 0.024 | 0.147 |
| **BCB-9635TJ** | 24 | 19/36 | 5 | 0.024 | 0.170 |
| **BCB-9636TJ** | 24 | 19/36 | 6 | 0.024 | 0.180 |
| **BCB-9641TJ** | 22 | 19/34 | 1 | 0.030 | 0.092 |
| **BCB-9642TJ** | 22 | 19/34 | 2 | 0.030 | 0.141 |
| **BCB-9643TJ** | 22 | 19/34 | 3 | 0.030 | 0.149 |
| **BCB-9644TJ** | 22 | 19/34 | 4 | 0.030 | 0.161 |
| **BCB-9645TJ** | 22 | 19/34 | 5 | 0.030 | 0.190 |
| **BCB-9646TJ** | 22 | 19/34 | 6 | 0.030 | 0.200 |
| **BCB-9651TJ** | 20 | 19/32 | 1 | 0.038 | 0.100 |
| **BCB-9652TJ** | 20 | 19/32 | 2 | 0.038 | 0.157 |
| **BCB-9653TJ** | 20 | 19/32 | 3 | 0.038 | 0.166 |
| **BCB-9654TJ** | 20 | 19/32 | 4 | 0.038 | 0.186 |
| **BCB-9655TJ** | 20 | 19/32 | 5 | 0.038 | 0.210 |
| **BCB-9656TJ** | 20 | 19/32 | 6 | 0.038 | 0.230 |
| **BCB-9661TJ** | 18 | 19/30 | 1 | 0.047 | 0.110 |
| **BCB-9662TJ** | 18 | 19/30 | 2 | 0.047 | 0.183 |
| **BCB-9663TJ** | 18 | 19/30 | 3 | 0.047 | 0.194 |
| **BCB-9664TJ** | 18 | 19/30 | 4 | 0.047 | 0.210 |
| **BCB-9665TJ** | 18 | 19/30 | 5 | 0.047 | 0.240 |
| **BCB-9666TJ** | 18 | 19/30 | 6 | 0.047 | 0.260 |

Cable Configurations up to 10 conductors.

\*Jackets can be made in all colors.