|  |
| --- |
| **UL1007/1569** |

|  |  |
| --- | --- |
|  | UL1007 PVC insulated general purpose electronic hook-up wire resistant to water, oil, acids, solvents and fungus. May be used for the internal wiring of electronic equipment. |
| |  |  | | --- | --- | | Conductor: | Tinned Copper | | Insulation: | PVC | | Temp Rating: | 80°C | | Voltage Rating: | 300 Volts R.M.S. | | Color Code | See Chart BCC-1 | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Nom. O.D. (in)** | **Nom. Insulation Thickness (in)** | **LBS/MFT** |
| **BW-5200-X** | 30 | 7 x 38 | 0.043 | 0.41 | 1.41 |
| **BW-5210-X** | 28 | 7 x 36 | 0.047 | 0.41 | 1.60 |
| **BW-5220-X** | 26 | 7 x 34 | 0.051 | 0.41 | 2.00 |
| **BW-5229-X** | 26 | Solid | 0.057 | 0.41 | 1.80 |
| **BW-5230-X** | 24 | 7 x 32 | 0.057 | 0.41 | 2.80 |
| **BW-5239-X** | 24 | Solid | 0.065 | 0.41 | 2.40 |
| **BW-5240-X** | 22 | 7 x 30 | 0.065 | 0.41 | 3.70 |
| **BW-5249-X** | 22 | Solid | 0.071 | 0.41 | 3.30 |
| **BW-5250-X** | 20 | 10 x 30 | 0.071 | 0.41 | 4.80 |
| **BW-5259-X** | 20 | Solid | 0.080 | 0.41 | 4.60 |
| **BW-5260-X** | 18 | 16 x 30 | 0.080 | 0.41 | 7.00 |
| **BW-5269-X** | 18 | Solid | 0.095 | 0.41 | 6.70 |
| **BW-5270-X** | 16 | 26 x 30 | 0.095 | 0.41 | 10.50 |

X = Color: See Page BCC-1