|  |
| --- |
| **AA-59569 Silver Plated Copper Tubular Braid** |

|  |  |
| --- | --- |
|  | Made in compliance with MIL-SPEC QQ-B-575 (as revised). Braid is formed so as to maintain coverage of 90% shielding, (70% for 0.78 and smaller), over the nominal diameters specified.  **Silver Plated:** Individual wires are silver plated copper wires, conforming to ASTM B298 standard, with 40 micro inches minimum of silver plating. Excellent for use at temperatures exceeding 200°C or where special resistance to corrosion is required |

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **Nominal Inside Diameter (inch)** | **AWG of Individual Ends** | **Carriers** | **# of Wires Per Strand** | **Total # of Individual Ends** | **Approximate AWG Equivalent** | **Approx. Current Carrying Cap. (amps)** |
| **BBD-10300T** | 0.031 | 36 | 24 | 1 | 24 | 22 | 7.0 |
| **BBD-10301T** | 0.062 | 36 | 24 | 2 | 48 | 19 | 11.0 |
| **BBD-10302T** | 0.062 | 34 | 16 | 2 | 32 | 19 | 11.0 |
| **BBD-10303T** | 0.062 | 32 | 16 | 1 | 16 | 20 | 9.0 |
| **BBD-10304T** | 0.078 | 36 | 24 | 3 | 72 | 18 | 16.0 |
| **BBD-10305T** | 0.109 | 36 | 24 | 4 | 96 | 16 | 19.0 |
| **BBD-10306T** | 0.109 | 34 | 16 | 4 | 64 | 16 | 19.0 |
| **BBD-10307T** | 0.109 | 32 | 16 | 2 | 32 | 17 | 18.0 |
| **BBD-10308T** | 0.125 | 36 | 24 | 5 | 120 | 15 | 25.0 |
| **BBD-10309T** | 0.125 | 34 | 24 | 3 | 72 | 16 | 19.0 |
| **BBD-10310T** | 0.125 | 32 | 24 | 2 | 48 | 15 | 25.0 |
| **BBD-10311T** | 0.156 | 36 | 24 | 10 | 240 | 12 | 40.0 |
| **BBD-10312T** | 0.171 | 36 | 24 | 7 | 168 | 14 | 32.0 |
| **BBD-10313T** | 0.171 | 34 | 24 | 5 | 120 | 13 | 36.0 |
| **BBD-10314T** | 0.171 | 32 | 24 | 3 | 72 | 14 | 32.0 |
| **BBD-10315T** | 0.203 | 36 | 24 | 13 | 312 | 11 | 46.0 |
| **BBD-10316T** | 0.203 | 34 | 24 | 8 | 192 | 11 | 46.0 |
| **BBD-10317T** | 0.203 | 32 | 24 | 5 | 120 | 11 | 46.0 |
| **BBD-10318T** | 0.250 | 36 | 24 | 16 | 384 | 10 | 53.0 |
| **BBD-10319T** | 0.281 | 30 | 24 | 5 | 120 | 9 | 60.0 |
| **BBD-10320T** | 0.375 | 36 | 48 | 8 | 384 | 10 | 53.0 |
| **BBD-10321T** | 0.375 | 34 | 48 | 5 | 240 | 10 | 53.0 |
| **BBD-10322T** | 0.375 | 32 | 48 | 3 | 144 | 11 | 46.0 |
| **BBD-10323T** | 0.375 | 30 | 24 | 7 | 168 | 8 | 75.0 |
| **BBD-10324T** | 0.437 | 30 | 24 | 10 | 240 | 6 | 90.0 |
| **BBD-10325T** | 0.500 | 36 | 48 | 11 | 528 | 9 | 62.0 |
| **BBD-10326T** | 0.500 | 34 | 24 | 7 | 336 | 9 | 62.0 |
| **BBD-10327T** | 0.500 | 32 | 48 | 4 | 192 | 9 | 62.0 |
| **BBD-10328T** | 0.500 | 30 | 48 | 15 | 360 | 5 | 120.0 |