|  |
| --- |
| **UL1429** |

|  |  |
| --- | --- |
|  | UL1429 is cross-linked PVC insulated general purpose electronic hook-up wire resistant to cut-through, abrasion, water, oils, acids, solvents and fungus. Resists shrink back and deformation when in direct contact with a soldering iron. |
| |  |  | | --- | --- | | Conductor: | Tinned Copper | | Insulation: | Irradiated PVC | | Temp Rating: | 80°C | | Voltage Rating: | 150 Volts R.M.S. | | |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Stranding** | **Nom. O.D. (in)** | **Nom. Insulation Thickness (in)** | **LBS/MFT** |
| **BW-5520-X** | 26 | 7 x 34 | 0.040 | 0.010 | 2 |
| **BW-5530-X** | 24 | 19 x 36 | 0.045 | 0.010 | 2 |
| **BW-5535-X** | 24 | 7 x 32 | 0.045 | 0.010 | 2 |
| **BW-5540-X** | 22 | 19 x 34 | 0.051 | 0.010 | 3 |
| **BW-5545-X** | 22 | 7 x 30 | 0.052 | 0.010 | 3 |
| **BW-5550-X** | 20 | 19 x 32 | 0.059 | 0.010 | 5 |
| **BW-5555-X** | 20 | 7 x 28 | 0.060 | 0.010 | 5 |
| **BW-5560-X** | 18 | 19 x 30 | 0.070 | 0.010 | 6 |
| **BW-5565-X** | 18 | 7 x 26 | 0.070 | 0.010 | 6 |
| **BW-5570-X** | 16 | 19 x 29 | 0.078 | 0.010 | 10 |

X = Color: See Page BCC-1