|  |
| --- |
| **SJOOW Cables** |

|  |  |
| --- | --- |
|  | SJOOW cables maintain excellent flexibility in cold temperatures. They are ozone, water and weather resistant. They have a high heat resistance as well as being resistant to oils, acids and chemicals. In addition, they are excellent to abrasion and cut resistance. |
| |  |  | | --- | --- | | Conductor: | Bare Copper | | Insulation: | Ethylene Propylene Diene Monomer Rubber (EPDM) | | Jacket: | Super Vu-Tron® III | | Temp Rating: | 105°C | | Voltage Rating: | 300 Volts R.M.S. | | Color Code Chart: | See Chart BCC-2 | | |

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Number of Conductors** | **Stranding** | **Insulation** | **Jacket (inches)** | **O.D. (Inches)** | **AMPS** |
| **BCB-8062** | 18 | 2 | 41 x 34 | 0.030 | 0.030 | 0.280 | 10 |
| **BCB-8063** | 18 | 3 | 41 x 34 | 0.030 | 0.030 | 0.300 | 10 |
| **BCB-8064** | 18 | 4 | 41 x 34 | 0.030 | 0.030 | 0.325 | 7 |
| **BCB-8072** | 16 | 2 | 65 x 34 | 0.030 | 0.030 | 0.305 | 13 |
| **BCB-8073** | 16 | 3 | 65 x 34 | 0.030 | 0.030 | 0.325 | 13 |
| **BCB-8074** | 16 | 4 | 65 x 34 | 0.030 | 0.030 | 0.350 | 10 |
| **BCB-8082** | 14 | 2 | 41 x 30 | 0.030 | 0.030 | 0.335 | 18 |
| **BCB-8083** | 14 | 3 | 41 x 30 | 0.030 | 0.030 | 0.360 | 18 |
| **BCB-8084** | 14 | 4 | 41 x 30 | 0.030 | 0.030 | 0.390 | 15 |