|  |
| --- |
| **SJOOW Cables** |

|  |  |
| --- | --- |
|  | SJOOW cables maintain excellent flexibility in cold temperatures. They are ozone, water and weather resistant. They have a high heat resistance as well as being resistant to oils, acids and chemicals. In addition, they are excellent to abrasion and cut resistance. |
| |  |  | | --- | --- | | Conductor: | Bare Copper | | Insulation: | Ethylene Propylene Diene Monomer Rubber (EPDM) | | Jacket: | Neoprene | | Temp Rating: | 90°C | | Voltage Rating: | 300 Volts R.M.S. | | Color Code: | See Chart BCC-2 | | |

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Blake Part Number** | **AWG** | **Number of Conductors** | **Stranding** | **Insulation** | **Jacket (inches)** | **O.D. (Inches)** | **AMPS** |
| **BCB-8362** | 18 | 2 | 16x30 | 0.030 | 0.030 | 0.280 | 10 |
| **BCB-8363** | 18 | 3 | 16x30 | 0.030 | 0.030 | 0.300 | 10 |
| **BCB-8364** | 18 | 4 | 16x30 | 0.030 | 0.030 | 0.325 | 7 |
| **BCB-8372** | 16 | 2 | 26x30 | 0.030 | 0.030 | 0.305 | 13 |
| **BCB-8373** | 16 | 3 | 26x30 | 0.030 | 0.030 | 0.325 | 13 |
| **BCB-8374** | 16 | 4 | 26x30 | 0.030 | 0.030 | 0.350 | 10 |
| **BCB-8382** | 14 | 2 | 41x30 | 0.030 | 0.030 | 0.335 | 18 |
| **BCB-8383** | 14 | 3 | 41x30 | 0.030 | 0.030 | 0.360 | 18 |
| **BCB-8384** | 14 | 4 | 41x30 | 0.030 | 0.030 | 0.390 | 15 |
| **BCB-8392** | 12 | 2 | 65x30 | 0.030 | 0.045 | 0.405 | 25 |
| **BCB-8393** | 12 | 3 | 65x30 | 0.030 | 0.045 | 0.425 | 25 |
| **BCB-8394** | 12 | 4 | 65x30 | 0.030 | 0.045 | 0.465 | 20 |
| **BCB-8302** | 10 | 2 | 104x30 | 0.045 | 0.060 | 0.540 | 30 |
| **BCB-8303** | 10 | 3 | 104x30 | 0.045 | 0.060 | 0.565 | 30 |
| **BCB-8304** | 10 | 4 | 104x30 | 0.045 | 0.060 | 0.625 | 25 |