|  |
| --- |
| **AMS-DTL-23053/12 CLASS 2** |

|  |  |
| --- | --- |
|  | M23053/12 is a PTFE heat shrink tubing. M23053/12 has the ability to withstand extreme heat and external chemicals, PTFE Shrink Tubing also boasts a low friction rating and a very low level of moisture absorption. M23053/12 has an operating temperature of -67C to 250°C and classes 1-4 have a 2:1 shrink ratio and class 5 has a 4:1 shrink ratio. |
| |  |  | | --- | --- | | MIL-DTL-23053/12 | | | UL Recognized | | | RoHS Compliant |  | | |

**Class 2 - Standard Wall – Shelf Life 4 Years**

|  |  |  |  |
| --- | --- | --- | --- |
| **Blake Part Number** | **Expanded I.D. (in)** | **Recovered I.D. Max (in)** | **Nom. Recovered Wall Thickness (in)** |
| **BT-1200-201-X** | 0.050 | 0.027 | 0.012 |
| **BT-1200-202-X** | 0.055 | 0.032 | 0.012 |
| **BT-1200-203-X** | 0.060 | 0.039 | 0.016 |
| **BT-1200-204-X** | 0.065 | 0.043 | 0.016 |
| **BT-1200-205-X** | 0.076 | 0.049 | 0.016 |
| **BT-1200-206-X** | 0.085 | 0.054 | 0.016 |
| **BT-1200-207-X** | 0.110 | 0.067 | 0.016 |
| **BT-1200-208-X** | 0.120 | 0.072 | 0.016 |
| **BT-1200-209-X** | 0.130 | 0.080 | 0.016 |
| **BT-1200-210-X** | 0.140 | 0.080 | 0.016 |
| **BT-1200-211-X** | 0.150 | 0.089 | 0.016 |
| **BT-1200-212-X** | 0.170 | 0.101 | 0.016 |
| **BT-1200-213-X** | 0.191 | 0.112 | 0.016 |
| **BT-1200-214-X** | 0.205 | 0.124 | 0.020 |
| **BT-1200-215-X** | 0.215 | 0.130 | 0.020 |
| **BT-1200-216-X** | 0.240 | 0.141 | 0.020 |
| **BT-1200-217-X** | 0.270 | 0.158 | 0.020 |
| **BT-1200-218-X** | 0.302 | 0.178 | 0.020 |
| **BT-1200-219-X** | 0.320 | 0.198 | 0.020 |
| **BT-1200-220-X** | 0.370 | 0.224 | 0.020 |
| **BT-1200-221-X** | 0.390 | 0.249 | 0.020 |
| **BT-1200-222-X** | 0.410 | 0.260 | 0.020 |
| **BT-1200-223-X** | 0.430 | 0.278 | 0.020 |
| **BT-1200-224-X** | 0.450 | 0.311 | 0.020 |
| **BT-1200-225-X** | 0.470 | 0.329 | 0.020 |
| **BT-1200-226-X** | 0.470 | 0.347 | 0.020 |
| **BT-1200-227-X** | 0.470 | 0.334 | 0.025 |
| **BT-1200-228-X** | 0.560 | 0.399 | 0.025 |
| **BT-1200-229-X** | 0.655 | 0.462 | 0.025 |
| **BT-1200-230-X** | 0.750 | 0.524 | 0.025 |
| **BT-1200-231-X** | 0.930 | 0.655 | 0.025 |
| **BT-1200-232-X** | 1.125 | 0.786 | 0.035 |
| **BT-1200-233-X** | 1.310 | 0.911 | 0.035 |
| **BT-1200-234-X** | 1.500 | 0.036 | 0.035 |

X = Color: See Page BCC-1