|  |
| --- |
| **MIL-I-631** |

|  |  |
| --- | --- |
| Macintosh HD:Users:martinweiner1:Desktop:31ZdzixIE5L.jpg | **Expandable Sleeving**products to a variety of industries. [Expandable Sleeving](http://www.awcwire.com/ProductTOC.aspx?id=Sleeving) offers an easy, affordable alternative to [heat shrink tubing](http://www.awcwire.com/ProductTOC.aspx?id=Heat-Shrink-Tubing). This type of sleeving is convenient because it adjusts to fit comfortably over wire and cable components without heat-shrinking. This saves you the hassle of dealing with the extra hassle and cost of heat shrink equipment  . |
| |  |  |  |  | | --- | --- | --- | --- | | Expandable Braided Polyester Sleeving | |  | **Specifications** | | Operational Temp. Range | -70°C to +125°C |  | MIL-I-631 | | |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **General Purpose Blake Part Number** | **Flame Retardant Blake Part Number** | **Minimum Supplied I.D. (in)** | **Maximum Supplied I.D. (in)** | **Nominal Wall Thickness (in)** |
| **BEBP-110-1/8** | **BEBP-120-1/8** | 0.093 | 0.250 | 0.25 |
| **BEBP-110-1/4** | **BEBP-120-1/4** | 0.125 | 0.437 | 0.25 |
| **BEBP-110-3/8** | **BEBP-120-3/8** | 0.187 | 0.625 | 0.25 |
| **BEBP-110-1/2** | **BEBP-120-1/2** | 0.250 | 0.750 | 0.25 |
| **BEBP-110-3/4** | **BEBP-120-3/4** | 0.500 | 1.250 | 0.25 |
| **BEBP-110-1 1/4** | **BEBP-120-1 1/4** | 0.750 | 1.750 | 0.25 |
| **BEBP-110-1 1/2** | **BEBP-120-1 1/2** | 1.000 | 2.500 | 0.25 |
| **BEBP-110-1 3/4** | **BEBP-120-1 3/4** | 1.250 | 2.750 | 0.25 |
| **BEBP-110-2** | **BEBP-120-2** | 1.500 | 3.000 | 0.25 |
| **BEBP-110-2 1/2** | **BEBP-120-2 1/2** | 1.750 | 3.500 | 0.25 |